## Slide 1: Structural Assessment of Historical Masonry structure
Student: Bc. Richard Šusták
Supervisor: doc. Dr. Ing. Luboš Podolka
Advisor: Ing. Carmen Amaddeo Phd.
Oponent: Ing. Robert Šinkner, MBA
6/2019

## Slide 2: Outline
Motivation
Aim of thesis
Study case – Description
Study case – Analysis 1.
Study case – Analysis 2.
Analysis results
Questions

## Slide 3: Motivation
Hot topic
Not well known in Czech Republic
Passion for architectural heritage
Cooperation on real project

## Slide 4: Aim of thesis
The aim of this master´s thesis is to perform a seismic evaluation before and after retrofitting of an historical masonry building located in seismic zone based on Italian code NTC 2008.
The chosen historical building is the “Palizzi” Castle located in the Reggio Calabria Province, Italy. The “Palizzi” castle is composed of a ground floor, first floor and under-roof level. The structure of the castle is mostly brick masonry with poor quality materials.
The Finite Element Model (FEM) of the structure has been built using SAP2000 software (Computers and Structures, Inc.), in particular it was performed a response spectrum analysis and also pushover analysis by using Etabs software (Computers and Structures, Inc.) of the structure. Results were verified and compared.
The outcome of this thesis will be comparison of linear and non-linear analysis on existing masonry structure with and without retrofitting.

## Slide 5: Study case – „Palizzi“ castle
Adress: Via Sant´Angelo, 14 Regio Calabria (RC) Palizzi, 89038, Italy
Name of building: „Palizzi“ castle
Permanent parcel: st. 113, 114
Building use: Historical monument
Owner: Municipality of Palizzi

## Slide 6: Study case – „Palizzi“ castle
Cadastral map of Palizzi municipality showing the location of the castle
Map of Italy with location of Palizzi town
(https://www.google.cz/maps/)

## Slide 7: Lay-outs:

## Slide 8: Sections:

## Slide 9: Photo-documentation

## Slide 10: Finite Element Model (FEM)
Archicad 21.
SAP 2000 v.19.3.

## Slide 11: Material Properties
Masonry typology | (N/mm²) | (N/mm²) | E (N/mm²) | G (N/mm²) | W (kN/m³)
Brick masonry and mortar | 2,52 | 0,60 | 1654 | 394 | 18
Masonry of brick and mortar (retrofitted) | 4.91 | 1.16 | 3225 | 768 | 18
Masonry typology |  |  | E (N/mm²) | G (N/mm²) | W (kN/m³)
Brick masonry and mortar | 2,52 | 0,60 | 1654 | 394 | 18
Masonry of brick and mortar (retrofitted) | 4.91 | 1.16 | 3225 | 768 | 18
Masonry typology | (N/mm²) | (N/mm²) | E (N/mm²) | G (N/mm²) | W (kN/m³)
Mixed masonry and mortar | 1,2844 | 0,0238 | 798 | 266 | 19
Masonry of brick and mortar (retrofitted) | 2,10 | 0,137 | 2497,5 | 999 | 19
Masonry typology |  |  | E (N/mm²) | G (N/mm²) | W (kN/m³)
Mixed masonry and mortar | 1,2844 | 0,0238 | 798 | 266 | 19
Masonry of brick and mortar (retrofitted) | 2,10 | 0,137 | 2497,5 | 999 | 19
Suggested properties based on historical sources and comparison
Suggested intervention properties
Material properties based on on-site experiments and tests.
Suggested intervention properties

## Slide 12: Analysis 1.: Response spectrum
Latitude = 37,9677, Longitude = 15,9875
Limit states
Collapse prevention Limit State (SLC)
Damage Limitation State (SLD)
Operating Limit State (SLO)
Life-Saving Limit State (SLV)
Usage Class = II
Nominal Life = 100
Spectrum Type = Elastic Horizontal
Soil Type = B
Topography Category = T1
Peak Ground Acceleration, ag /g -

## Slide 13: Analysis 1.: Loads
12. load combinations
1. envelope
Roof and slabs – with and without
SRSS - Square Root of Sum of Squares

## Slide 14: Analysis 1.: Results - URM
 | S22 | 
Max stress | 9,254 N/mm² | 1,28 N/mm²
Average stress | 0,587642 N/mm² | 1,28 N/mm²
Min stress | 0,007884 N/mm² | 1,28 N/mm²
 | S22 | 
Max stress | 9,254 N/mm² | 1,28 N/mm²
Average stress | 0,587642 N/mm² | 1,28 N/mm²
Min stress | 0,007884 N/mm² | 1,28 N/mm²
Model without slabs – direct stress
S22: Direct stress (force per unit area) acting on the positive and negative 2 faces in the 2-axis direction.
: Tensile strength of masonry (N/mm²)
Model without slabs – shearing stress
 | S12 | 
Max stress | 7,516 N/mm² | 0.0238 N/mm²
Average stress | 0,405414 N/mm² | 0.0238 N/mm²
Min stress | 0,0005604 N/mm² | 0.0238 N/mm²
 | S12 | 
Max stress | 7,516 N/mm² | 0.0238 N/mm²
Average stress | 0,405414 N/mm² | 0.0238 N/mm²
Min stress | 0,0005604 N/mm² | 0.0238 N/mm²
S12: Shearing stress (force per unit area) acting on the positive and negative 1 faces in the 2-axis direction and acting on the positive and negative 2 faces in the 1-axis direction.
: Shear strength of masonry (N/mm²)

## Slide 15: Analysis 1.: Results - RM
Retrofitted model with slabs – direct stress
S22: Direct stress (force per unit area) acting on the positive and negative 2 faces in the 2-axis direction.
: Tensile strength of masonry (N/mm²)
 | S22 | 
Max stress | 11,439 N/mm² | 2,1 N/mm²
Average stress | 0,433839 N/mm² | 2,1 N/mm²
Min stress | 0,001775 N/mm² | 2,1 N/mm²
 | S22 | 
Max stress | 11,439 N/mm² | 2,1 N/mm²
Average stress | 0,433839 N/mm² | 2,1 N/mm²
Min stress | 0,001775 N/mm² | 2,1 N/mm²
Retrofitted model with slabs – shearing stress
 | S12 | 
Max stress | 3,557 N/mm² | 0.137 N/mm²
Average stress | 0,258344 N/mm² | 0.137 N/mm²
Min stress | 0,002053 N/mm² | 0.137 N/mm²
 | S12 | 
Max stress | 3,557 N/mm² | 0.137 N/mm²
Average stress | 0,258344 N/mm² | 0.137 N/mm²
Min stress | 0,002053 N/mm² | 0.137 N/mm²
S12: Shearing stress (force per unit area) acting on the positive and negative 1 faces in the 2-axis direction and acting on the positive and negative 2 faces in the 1-axis direction.
: Shear strength of masonry (N/mm²)

## Slide 16: Analysis 1: Verification and conclusion
Chart: 
| S 22 | S 12 | S 22 after retrofitting | S 12 after retrofitting
Percentage of verified results | 90.4528 | 0.3773 | 98.7205 | 37.8609

## Slide 17: Analysis 2.: Pushover analysis
Finite element model
Hinges
Lateral load
Verification methods
- Base shear
- Target displacement

## Slide 18: Analysis 2.: Base shear results - URM
X - DIRECTION
Y - DIRECTION

## Slide 19: Analysis 2.: Base shear results - RM
X - DIRECTION
Y - DIRECTION

## Slide 20
Analysis 2.: Target displacement - URM
X - DIRECTION
Y - DIRECTION

## Slide 21
Analysis 2.: Target displacement - URM
X - DIRECTION
Y - DIRECTION

## Slide 22: Analysis 2.: Verification
FE model reference | Direction | Fy* | dy* (mm) | dt* (mm)
URM | X | 3,266 | 18,307 | 2,917
 | Y | 2,283 | 26,002 | 4,67
RM | X | 5,405 | 23,436 | 4,952
 | Y | 4,706 | 32,494 | 6,141
dy*: yield displacement
Fy*: yield force
dt*: target displacement

## Slide 23: Thank you for your attention!
I want to acknowledge “Studio KR e Associati” and “Studio Associato Amaddeo-Fiumanò” for providing the blueprint and the design specification of the castle.

## Slide 24: Questions:
Supervisor: doc. Dr. Ing. Luboš Podolka
Jak by bylo možno počítanou historickou stavbu zabezpečit vůči účinkům zemětřesení ?
Počítá majitel objektu s ponecháním stavby ve stávajícím stavu bez střechy a s poškozenými stropními konstrukcemi, nebo bude nějakým způsobem stavba opravena ?
Oponent: Ing. Robert Šinkner, MBA.
Jakou metodou byl objekt zaměřen? Laserovým skenováním nebo klasickými geodetickými metodami?
Jak jste se dostal k takové zajímavé mezinárodní spolupráci?

## Slide 25: Retrofitting methods
Bamboo-Band retrofitting technique
Reinforced plaster
Shotcrete
Fiber-Reinforced polymer (FRP)
      Post-tensioning
      Confinement
      Center core
      Injection

## Slide 26: Experiment - NHERI@UCSD